| Material | Appearance | Temperature | Life at 100 rpm | Advantages | Application |
| --- | --- | --- | --- | --- | --- |
| Tygon | Clear | -50 to 74°C | 300 hours | Clear and Economical | Acids, Alkalies, Viscous Fluids |
| Tygon LFL | Clear | -50 to 74°C | 300 hours | Pharmaceutical Grade. Longest Flex Life Of All Tygon | Acids, Alkalies Viscous Fluids, Pharmaceuticals |
| Silicone (Peroxide cured) | Translucent | -60 to 260°C | 800 hours | Excellent Biocompatibility | Sterile Fluids |
| Silicone (Platinum cured) | Translucent | -60 to 260°C | 800 hours | Very Low Leaching of Organic Compounds | Sterile Fluids |
| Norprene | Opaque, Black | -50 to 130°C | 1400 hours | Long Life | Acids, aAkalies, General Purpose |
| Viton | Opaque, Black | -20 to 205°C | 160 hours | Resists Most Chemicals | Acids,Alkalies, solvents, Viscous Fluids |
| PharMed | Opaque, Beige | -50 to 130°C | 1400 hours | Pharmaceutical Grade | Acids, Alkalies, Sterile Fluids, Viscous Fluids |

Tube   Material